# Vitronexa Carbon – Pelletized Activated Carbon (Pelletized Carbon)

“Ultrafine Purity. Fast Response. Global Standards”.

# About Vitronexa Carbon

Vitronexa Carbon is a specialized manufacturer of premium-grade activated carbon engineered for demanding purification processes. Our Pelletized Carbon is developed from carefully selected coconut shell charcoal using steam activation and micron-level grinding — delivering consistent performance, rapid adsorption, and full regulatory compliance.

# What is Pelletized Carbon and How It Works
Pelletized Activated Carbon (Pelletized Carbon) is a high-density, extruded adsorbent engineered for gas-phase applications. With uniform cylindrical pellets and controlled pore structure, it delivers excellent adsorption capacity for volatile organic compounds (VOCs), solvent vapors, odors, and toxic gases.

# At Vitronexa, Pelletized Carbon is manufactured under dust-controlled conditions with consistent hardness and low pressure drop, making it ideal for use in air purification units, industrial gas treatment, solvent recovery, respirators, and emission control systems. Its durability and uniformity ensure reliable performance across demanding air and gas filtration application

Key Functional Benefits:

- Cylindrical pellet form ensures low-pressure drop-in air and gas systems

- High CTC adsorption capacity for effective removal of VOCs, odors, and toxic gases

- Excellent mechanical strength for long service life and multiple regeneration cycles

- Uniform particle size for consistent airflow and performance stability

| Technical Parameter | Specification Range | ASTM- Standards |
| --- | --- | --- |
| CTC | Min 60% | ASTM D3467 |
| Surface Area (m²/g) | 1000 – 1150 m²/g | ASTM D6556 |
| Mesh Sizes Available | 2mm, 3mm, ,4mm | ASTM D2854 |
| Moisture Content | Max 5% | ASTM D2867 |
| Apparent Density | 480 – 520 kg/m³ | ASTM D2854 |
| Ash Content | Max 4% | ASTM D2866 |
| Hardness Number | Min 98% | ASTM D3802 |

Custom values available on request. Each batch is traceable and COA-certified.

🔷 Major & Essential Applications

Industrial Air Purification

- Removal of VOCs, odors, and hazardous air pollutants

- Emission control in manufacturing facilities

- Gas stream purification in chemical and process industries

💨 Gas Processing & Refining

- Purification of hydrogen, nitrogen, and natural gas

- Removal of hydrogen sulfide (H₂S), siloxanes, and organic vapors

- Solvent vapor recovery and protection of downstream equipment

🏭 Environmental Odor Control

- Odor removal in wastewater treatment facilities

- VOC capture from industrial exhausts

- Air purification in composting and waste management plants

⚗ Chemical & Pharma Gas Purification

- Trace contaminant removal in process gases

- Catalyst protection through impurity adsorption

- Purification of CO₂, ammonia, and specialty gases

🔷 Why Choose Vitronexa Pelletized Carbon?

- ✔ High CTC adsorption capacity (ASTM D3467)

- ✔ Ultra-low dust, ensuring clean handling and system stability

- ✔ Excellent mechanical strength for longer service life

- ✔ Consistent pellet size for low pressure drop and uniform airflow

- ✔ Custom pellet diameters (2 mm, 3 mm, 4 mm) available

- ✔ Full CoA, MSDS, and batch QC reports provided

🔷 Pelletized Carbonkaging & Logistics

Standard Pelletized Carbonkaging:

- 25 kg bags

- 50 Kg Pags

- 500 kg jumbo bags (FIBC)

🔷 Certifications & Documentation

- NSF Certified for drinking water applications

- ISO 9001:2015 Quality Management Certified

- Hala Certified

- Kosher certified

- MSDS, CoA, and Test Reports included per batch

- Certificate of Analysis (CoA) and third-party test reports issued for every production batch

- Compliant with ASTM D5029 & D3838 testing protocols

🔷 Contact & Brochure Access
📩 sales@vitronexa.com / info@vitronexa.com	
📞 +91-9941172345, 
🌐 www.vitronexacarbon.com
📍2/135 karim Nagar periyar street palavakkam

Chennai - 600041